# PRODUCT SPECIFICATIONS

Sealing of joints in structures with pre-compressed permanently elastic multi-functional tape.

Item	.....	Preliminary treatment of the subsurface

Clean the joint surface mechanically. The subsurface needs to be dry, free of dust, loose bits, oils, greases or other contaminations which could act as release agent. Joint tolerances of over 50% of the lowest value are to be leveled out in a suitable manner.

............rm.	Price ............ €	Total Price ............ €

Item	.....	Sealing

Delivery and installation of a permanently elastic, multi-functional tape, pintaband 3complete Plus, according to DIN 18 542 BG 1, self-adhesive on one side, pre-compressed ex-factory. Manufactured and tested according to the quality standards DIN EN 18542 and DIN 4102. Impregnated with a polyacrylate causing a delayed recovery.
The sealing tape is compatible with all common building materials.

The tape possesses the following qualities:

- Free of plasticizers(softening agents), heavy metal, chlorine, bitumen, fibers, CFC, formaldehyde, PCB and emissions

- Fire class B1 according to DIN 4102

- BG 1 / BG R according to DIN 18542

- Water vapor permeable and sound absorbing

The tape is delivered on rolls, over 20% pre-compressed and correctly dimensioned according to the joint width. An installation not complying with the predefined recommendations is not permitted.

Tape width at least twice the pre-compressed tape thickness,

smallest joint width = tape thickness

Tape dimensions (joint tolerance):  	          mm	width:     mm

Example: manufacturer

pinta abdichtung GmbH

The manufacturer´s instructions are to be observed.

............rm.	Price ............ €	Total Price............ €